## Slide 1: Photorefractive Nonlinearity
Dynamic Holography

## Slide 2
Courtesy of Marinova, et al. Wiley Encyclopedia of Electrical and Electronics Engineering, (2016)

## Slide 3
Courtesy of Marinova, et al. Wiley Encyclopedia of Electrical and Electronics Engineering, (2016)

## Slide 4
Gain Coefficient
Photorefractive Equations of Kukhtarev et al. (1977)

## Slide 5
10.5 Photorefractive Equations of Kukhtarev et al.
Assume that the crystal contains NA acceptors and ND0 donors per unit volume, with NA<<ND0
Rate equations :
where, s : photoionization cross section of a donor
b : thermal generation rate (thermal ionization)
g : recombination coefficient
j : electrical current density
(10.5.1)
(10.5.2)
R. W. Boyd, 3rd ed.

## Slide 6
Electrical current density :
where, m : electron mobility
D : Diffusion constant
jph : photovoltaic contribution to the current
Local field within the crystal :
Change in dielectric constant :
Wave equation for the optical field :
: Cannot easily be solved exactly
(10.5.3)
(10.5.4)
(10.5.5)
(10.5.6)
To Convert to SI:
Replace 4π with 1/0
everywhere

## Slide 7
10.6 Two-Beam Coupling in Photorefractive Materials
Optical field within the crystal :
Intensity distribution of light within the crystal :
where,
: grating wave vector
(10.6.2)

## Slide 8
Intensity distribution of light within the crystal can also be described by
where,
: modulation index
Approximate steady-state solution (|I1|<<I0)
Put,
1) From x independent term,
(10.6.5)
Report

## Slide 9
In most realistic case,
2) From eiqx dependent term (assume E0=0),
where,
: diffusion field strength
: maximum space charge field
Report
: Einstein relation

## Slide 10
i) Quarter period shift of the index grating with respective to the intensity distribution
ii)
iii)
: depends also on grating vector q
(10.6.8)
Defining the optimum value of q maximizing the second factor as qopt,
where,
can be adjusted

## Slide 11
(10.6.2) and (10.6.8) 
where,
Nonlinear polarization :
Dielectric constant change :
(10.6.16)
1) Steady state

## Slide 12
Wave equation (slow varying approx.) :
where,
Similarly,
: when G>0, Is is amplified and Ip is attenuated

## Slide 14
Beam Fanning

## Slide 15: Spatula Laser!
Applications of Optical Phase Conjugation
David M. Pepper
Scientific American
Vol. 254, No. 1 (January 1986), pp. 74-83